## Slide 1
ENCOR 446 CS sales tool

## Slide 2: ENCOR 446 CS basic data
ENCOR 446 CS is a very low surfactant styrene acrylic latex for use in various construction and adhesive applications. It is useful in applications such as water-resistant construction adhesives and cement admixtures.
ENCOR® 446 CS features high dry-film adhesion to a variety of substrates, including low energy surfaces, and yields tough, flexible films. In addition, it has high solids (62%) and quick water release for fast drying.
Basic data
  Appearance： Milky white
  S.C.： 62%
  PH ： 6
  P.S.(um)： 0.3
  Viscosity (Brookfield, cP) <1000
  Tg ℃ 12
  MFFT ℃ 6
Typical applicatoin
  2K waterproofing mortar
  Interface agent
  Repair mortar
  CTA

## Slide 3
Liquid part |  |  | 
ENCOR 446 |  | 22 | 
Water |  | 77.7 | 
Foamaster NXZ |  | 0.3 | 
Powder part： |  |  | 
P.O 42.5 cement |  | 45 | 
Sand（70-140mesh） |  | 42.6 | 
CaCO3（325mesh） |  | 12.5 | 
M10 |  | 0.12 | 
F10 |  | 0.2 | 
L:P |  | 9:25 | 
 |  | Results | JC/T 2090 I
Bonding strength/Mpa | Normal | 1.25 | ≥0.7
 | Alkali treatment | 1.32 | ≥0.7
 | Water treatment | 1.26 | ≥0.7
Flexural strength/MPa |  | 10.8 | ≥4
Compressive strength/MPa |  | 28 | ≥12
JC/T 2090 starting formulation （9:25）

## Slide 4
JC/T 984 starting formulation（3:10）
 |  | With CACO3 | 
Liquid part： |  |  | 
ENCOR 446 |  | 32 | 
Water |  | 67.8 | 
Foamaster NXZ |  | 0.2 | 
Powder part： |  |  | 
P.O 42.5 cement |  | 45 | 
Sand （70-140mesh） |  | 35 | 
CaCO3（325目） |  | 20 | 
M10 |  | 0.05 | 
F10 |  | 0.3 | 
L:P |  | 3:10 | 
 |  | Results | JC/T 984 I
Flowability/cm,0min |  | 26 | /
Bonding strength/Mpa | 7d | 1.98 | ≥0.8
 | 28d | 2.25 | ≥1
Compressive strength/MPa |  | 45.8 | ≥18
Flexural strength/MPa |  | 12.1 | ≥6
Water absorption/% |  | 3.81 | ≤6

## Slide 5: ENCOR 446 CS water absorption
L:P=3:10 P:C=0.13
Chart: Water absorption/%
| ENCOR 5525 CS | ENCOR 446 CS | PS 608
24h | 4.03 | 3.19 | 7.43
48h | 4.62 | 3.81 | 8.66

## Slide 6: ENCOR 446 CS strength performance
Chart: Bonding strength
| ENCOR 5525 | ENCOR 446 | PS 608
7d | 1.86 | 1.88 | 1.83
28d | 2.4 | 2.46 | 2.34
Chart: Compressive/Flexural strength
| ENCOR 5525 | ENCOR 446 | PS 608
Compressive strength | 37.1 | 33.6 | 34.7
Flexural strength | 10.8 | 11.4 | 13.2
L:P=3:10 P:C=0.13

## Slide 7
JC/T 984 starting formulation（3:10）
 |  | Without CACO3 | 
Liquid part： |  |  | 
ENCOR 446 |  | 27 | 
Water |  | 72.7 | 
Foamaster NXZ |  | 0.3 | 
Powder part： |  |  | 
P.O 42.5 cement |  | 50 | 
Sand（70-140mesh） |  | 50 | 
M10 |  | 0.06 | 
F10 |  | 0.25 | 
L:P |  | 3:10 | 
 |  | Results | JC/T 984 I
Flowability/cm,0min |  | 30.5 | /
Bonding strength/Mpa | 7d | 1.77 | ≥0.8
 | 28d | 2.02 | ≥1
Compressive strength/MPa |  | 36.6 | ≥18
Flexural strength/MPa |  | 13.2 | ≥6
Water absorption/% |  | 4.43 | ≤6

## Slide 8
JC/T 984 starting formulation（1:4）
 |  | Without CaCO3 | With CaCO3 | 
Liquid part： |  |  |  | 
ENCOR 446 |  | 35 | 35 | 
Water |  | 64.7 | 64.7 | 
Foamaster NXZ |  | 0.3 | 0.3 | 
Powder part： |  |  |  | 
P.O 42.5 cement |  | 45 | 40 | 
Sand（70-140mesh） |  | 54.7 | 50 | 
CaCO3（325mesh） |  | 0 | 9.7 | 
M10 |  | 0.04 | 0.04 | 
F10 |  | 0.3 | 0.3 | 
L:P |  | 1:4 |  | 
 |  | Results |  | JC/T 984 I
Flowability/cm,0min |  | 133 | 135 | /
Bonding strength/Mpa | 7d | 1.38 | 1.37 | ≥0.8
 | 28d | 1.37 | 1.52 | ≥1
Compressive strength/MPa |  | 30 | 31.4 | ≥18
Flexural strength/MPa |  | 11.9 | 12.3 | ≥6
Water absorption/% |  | 5.7 | 5.84 | ≤6

## Slide 9: ENCOR 446 CS for CTA application
 | 30% ENCOR 446 | 35% ENCOR 446 | 30% Styrofan ECO 7623
Bonding strength/MPa | 1.05 | 1.3 | 1.21
Bonding strength after water treatment/MPa | 0.97 | 1.28 | 1.05